## Slide 1
肯纳曲轴连杆高效切削的解决方案
发动机领域

## Slide 2: 公司简介
深厚积淀，进取精神
Notes: Kennametal 公司，始建于 1938 年的技术创新，我们一直在不断地推陈出新。
2002 年，我们收购了一家创建于 1925 年的 WIDIA 公司。事实上，我们收购 Greenfield Tap & Die 之后，我们最早的品牌可追溯至 1848 年。
我们首先在宾夕法尼亚州拉特罗布打开了大门，我们的全球总部也设在那里。今天，Kennametal 业已成为一家全球性公司，我们在北美地区以外实现的销售额超过总额的 50%。
我们凭借着雄厚的技术底蕴，推动业务走出国门，走向世界。
我们的公司发展依靠的是扎实的基础和创业思维。
2013 年，我们从 ATI 收购了钨材料业务。此次收购进一步增强了我们的模具产品组合，加快了我们的先进碳化钨设施开发计划，促使我们在关键增长市场的发展，包括航空航天、能源及相关工艺产业。

## Slide 3: 曲轴加工
曲轴加工刀具简介
曲轴加工通用类刀具
曲轴加工特有工序
    车车拉
    车拉
    外铣
    内铣

## Slide 4
曲轴刀具综合解决方案
„Hollow-Mill“-Cutter
粗加工法兰式结构
大直径粗加工刀体
车拉刀具
适合粗精加工
应用多个曲轴回转中心
深孔钻削
应用于20至30倍直径比深的内孔加工
加工铸铁和钢件类材料
Dodeka / Octacut
曲轴端面的铣削
内铣刀体
轴承档的粗精加工
外铣刀体
轴承档的粗精加工
车车拉刀具
应用中心回转轴承的粗精加工
HSC Auto Speed VME 195
全自动检测外铣刀体
全自动检测车车拉刀体
车削刀具
粗精加工法兰结构
具有直径变幻的粗精加工刀具形式
行业解决方案 – 精加工
保证最小跳动的调节方式
行业解决方案 – 粗加工
较高的生产效率
较好的灵活性
行业解决方案 – 粗加工
较高的生产效率
较好的灵活性

## Slide 5: 曲轴通用类刀具概述
铣削两端面和中心孔加工
车削
钻削，铰削和攻丝法兰面孔系
油孔加工

## Slide 6: 曲轴通用类刀具概述
铣削两端面和中心孔加工

## Slide 7: 曲轴通用类刀具概述
首选---分体式结构
可调整刀夹
最大的铁屑排屑空间
内冷支持
维修简便
通用性广

## Slide 8: 曲轴通用类刀具概述
整体式结构
可微量调整
最强的刀具刚性
最多的刀齿分布
内冷支持

## Slide 9: 曲轴通用类刀具概述
HSK100A
直径D87-D41
Z=2
可调整刀夹
刀片1*SPPX09T308
刀片2*SPPX120412
切削钢件
切削速度：Vc=150m/min
进给： fz=0.2mm

## Slide 10: 曲轴通用类刀具概述
HSK100A
直径D30-D40
Z=2
4个可调整刀夹
刀片4*SPPX120408
切削钢件
切削速度：Vc=150m/min
进给： fz=0.2mm

## Slide 11: 曲轴通用类刀具概述
HSK100A
直径D85
Z=3（端面Z=1）
整体式结构
刀片SNMU120612
切削钢件

## Slide 12
适用性
加工时间
刀具结构复杂
加工公差
-
单独的车车拉生产线
车车拉 + 外铣复合
车车拉 + 内铣复合
TTB
ID
OD
适用性
加工时间
刀具结构复杂
加工公差
曲轴优化生产线
车车拉 + 外铣复合
适用性
加工时间
刀具结构复杂
加工公差
重载粗加工
车车拉 + 内铣复合
适用性
加工时间
刀具结构复杂
加工公差
适用于大批量生产相同类型的曲轴
只加工主轴承档
曲轴轴径类刀具

## Slide 13
粗加工:
- 切削速度.: 140 ... 200 m/min
- 进给量: 0,25 ... 0,5 mm-1
精加工:
- 切削速度.: 160 ... 220 m/min
- 进给量: 1800 ... 2400 mm/min
最快的加工方式
高性能硬质合金牌号
车拉刀具

## Slide 14
车车拉刀具
粗加工:
- 切削速度: 140 ... 200 m/min
- 进给量: 0,25 ... 0,5 mm-1
精加工:
- 表面质量: Rz 4 ... 6 µm
-切削速度.: 160 ... 220 m/min
-进给量: 1800 ... 2400 mm/min
改进的系统
尽可能的 ISO 标准刀片
高性能的硬质合金牌号

## Slide 15
车车拉刀具刀夹

## Slide 16
主轴颈加工
车车拉刀具刀夹

## Slide 17
车车拉刀具刀夹
主轴颈加工

## Slide 18
车车拉刀具刀夹
Notes: Innovation is at the heart of Kennametal’s competitive advantage
In locations including Latrobe, Bedford, Rogers and Evans in the US and Fürth in Germany and Bangalore in India we have more than a thousand research scientists and development engineers
  Using a stage gated process, ACE, we focus on customer needs to design products that will make our customers more productive
  Focused on customer needs
  Developing new cutting tool & wear resistant materials
  Designing products to make our customers more productive
  We emphasize and reward employees who create patentable innovation
  Kennametal named a Best-Practice Partner by the APQC
  for outstanding practices in innovation. After surveying 100 major corporations in the United States known for their innovation, Kennametal was recognized for efficiencies in ACE, and the company’s overall definition of innovation.

## Slide 19
快换式内铣刀结构
内铣刀体操作简易
优势：
夹紧环是仅有的一种附件
可以进行手动换刀（刀具重量在9~14KG）
换刀装卸装置
刀盘
夹紧环
刀具

## Slide 20
HNK韩国
内径 = 1250 mm
宽 = 75 mm
内铣刀具

## Slide 21
刀片的排列是有很多种不同的摆放形式
在刀片排列中必须要考虑到铁屑的排出
在刀片排列设计中多齿的刀体上必须考虑有足够大的容屑空间
每个不同的项目都必须依据其特殊要求而设计
内铣刀具

## Slide 22
粗加工:
- 切削速度.: 180 ... 250 m/min
- 铁屑厚度: 0,25 ... 0,30 mm
精加工:
-切削速度.: 200 ... 350 m/min
-铁屑厚度: 0,15 … 0,22 mm
超密齿刀体
高精度
高精度结构（带调整选项）
HEINLEIN
外铣刀具

## Slide 23
刀夹设计
轴向固定:
- 基准面磨削
较高重复定位精度
较小的跳动值
径向固定:
- 内六角 M10
- 清洁简便
- 操作顺手
- 标准螺钉
切线方向:
- 销钉
- 可靠的夹紧方式
HEINLEIN
刀夹
刀体
夹持
外铣刀具

## Slide 24
直径 = 1150 mm
宽 = 75 - 120 mm
MHI (1573555)
外铣刀具

## Slide 25: 连杆

## Slide 26
加工工艺
毛坯
2端面加工
大小头的粗加工
小头的精加工
螺栓孔加工
涨断/切断
合盖装配
大/小头精加工
小头压套

## Slide 27
铣削止推面

## Slide 28
HSK80C shell mill arbor with exchange lock
M780 milling cutter Ø100; z=12 + 3
3x Finishing insert SNXF1204ZNSNGP TN7525
12x Roughing insert SNXF120412SNGP TN7525
Offset of wiper insert 0,02 mm
The Solution:
Surface finish Rz 5 - 6
The Results:
D = 100 m/min
Vc = 180 m/min
Vf = 1030 mm/min
FPT = 0,12 mm
DOC = 1,7 – 2,0 mm
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Milling thrust faces
Coolant: no
Machine: Transferline
Objective: Achieve surface finish Rz 16
The Task:
铣削止推面案例
STEEL

## Slide 29
DWG 1552204
HSK63A Special Topcut Plus
Chamfering 0,7 x 30o both sides
Insert for drilling XOMT070304-34 TN7015
Insert for chamfering 3xCCMT060204-11 KT315
Insert for chamfer adjustable
4 useable cutting edges
The Solution:
Quite run without vibrations
The Results:
D = 22 mm
Vc = 160 m/min
Vf = 302 mm/min
FPT = 0,13 mm/rev
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Drilling into solid material
Coolant: Yes
Machine: M/C with 4 spindles
Objective: Drilling Ø22 and chamfering forward and backwards
The Task:
小头孔加工案例
STEEL

## Slide 30
Component:Conrod
Material: C70S6
Operation:Semi-Finsih Conrod Big Eye
Coolant: Yes (With Internal Coolant)
Equipment: Doosan (VMC BT40)
2 Inserts for rough boring(D47.7mm) and circular mill back chamfer (SCMT09T308MP KCP25)
1 Insert for Semi-Finishing(D49.4) with Adjusting element(SCMT09T30811 KT315)
1 Insert for Chamfer (SCMT09T308MP KCP25)
Vc= 200 m/min(Boring)
230m/min(Milling Chamfer)
D = D47.7/49.4 mm; Z = 2+1+1
Fz = 0.15 mm/rev(Rough)
=0.1 mm/rev(Semi-Finish)
=0.12 mm/rev (Circular Mill Chamfer)
大头孔加工案例
4 Operation in 1 tool, Reduce Cycle Time.
Take full advantage of rough insert two cutting edge, One for rough boring, another for circular mill, 4 usages per insert, low cost.
Good Suface quality, better than Ra1.6
DWG:2704052
STEEL
The Solution:
The Results:
The Data:
The Task:

## Slide 31
DWG 1552203
D = 46,5 / 48,5 mm; z = 3
Vc = 146 m/min
Vf = 600 mm/min
Fz = 0,2 mm
Component: Pass. car conrod
Material:C70 S6 BY
Operation: Rough and Semi-finish Big Eye
Coolant: Yes
Machine: M/C with 4 spindles
Objective: Big Eye Ø 48,5 0/+0,05
The Task:
HSK63A special boring with special cartridge
Rough insert 3x SCMT09T308-MU TN8025
Semi-finish insert 3x SCMT09T308-11 HT93VX(Cermet)
Two side chamfer(circular mill back chamfer) insert 3x CCMT060204-11 KT315
Special cartridge for chamfer, Adjustalbe
The Solution:
Good chip control
The Results:
The Data:
STEEL
大头孔加工案例
Notes: Insert grades are important
Semi fin is cermet

## Slide 32: 螺孔加工

## Slide 33
DWG 1552198
STEEL
铣削螺纹孔面
Component: Pass. car conrod
Material: C70S6BY
Operation: Spot Facing For Screw Holes
Coolant: Yes
Machine: M/C with 4 spindles
The Task:
Assembly with Weldon Adaptor
S.C Endmill
Stock: 2mm
Z=4/2(Center Cutting)
Grade KC7315
Internal Coolant
The Solution:
Good Surface Roughness
The Results:
The Data:
Vc=73m/min
Z=4
Fz=0.25mm/r

## Slide 34
铣削螺纹孔面
Component: Pass. car conrod
Material: Powder Metal
Operation: Spot Facing For Screw Holes
Coolant: Yes
Machine: M/C with 2 spindles
The Task:
D25 Mill1-10 “25A04R32M12ED10”
Insert 4x EPT10T331PDSRGE KCPK30
Adaptor HSK63AST12084M
Internal Coolant
The Solution:
Good Surface Roughness
The Results:
The Data:
Vc=125m/min
Z=4
Fz=0.12mm/r
Powder Metal

## Slide 35
DWG 1523674
D = 8,6 mm
Vc = 140 m/min
Vf = 1036 mm/min
FPT = 0,2 mm/rev
Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Drilling screw hole
Coolant: Yes
Machine: M/C with 4 spindles
Objective: Drilling with high speed
The Task:
HSK63A Hydraulic chuck
Solid carbide drill with HP geometry
Point angle 140 degree
Typ B256 B751A1523674 KC7315
4 guiding lands
Internal coolant
The Solution:
Double cutting speed
The Results:
螺孔钻削
STEEL

## Slide 36
攻丝
D = 8 mm
Vc = 15 m/min
Fz = 1 mm/r
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Tap M8x1
Coolant: Yes
Machine: M/C with 4 spindles
Objective: Tapping,2x Retract Speed
The Task:
HSK63A Syncro Chuck
HSS-PM Tap, FX.006060
TiCN Coating
Coolant via bigger sealing disc
The Solution:
Good Chip Flute Control
The Results:
STEEL
Notes: Bass company, tap

## Slide 37
HSK63A Whistle Notch adapter
Brush with Ø75 width 25 mm
Cordwire dia. 0,38
The Solution:
D = 75 mm
Vc = 500 m/min
Vf = 1060 mm/min
Fz = 0,5 mm/rev
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Brushing
Coolant: Yes
Machine: M/C with 4 spindles
Objective: Deburring tap hole exit
The Task:
刷孔去毛刺
STEEL

## Slide 38: 背面孔加工
Pilot Cutting
D 6.8 8.7 mm
Vc 43 55 m/min
Z 2 2
Fz 0.18 0.075 mm/r
The Data:
Component: Pass. car conrod
Material: Powder Metal
Operation: Back Countersinking
Coolant: Yes
Machine: M/C with 4 spindles
The Task:
Special Slim Hyd. Chuck DWG1998444
S.C Countersink with Pilot DWG2656121(to guide the tool in the
Hole previously machined from the opposite side)
The Solution:
No vibrations in spite of the long overhang
The Results:
Powder Metal

## Slide 39
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Drilling Oil Hole
Coolant: Yes
Machine: HMC
The Task:
HSK63A Hydraulic chuck
Standard 30XD Deep Hole Drill B274Z04000HPG KC7425
4 guiding lands
Internal coolant
Pilot drill(B977A04000 KC7315)
The Solution:
High Speed
Good Chip Control
The Results:
油孔加工
D = 4 mm
Vc = 70 m/min
FPT = 0,12 mm/rev
Z=1
STEEL

## Slide 40
铣槽加工
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Mill Locating Groove and Debug
Coolant: Yes
Machine: M/C with 4 spindles
The Task:
D21.7 Grooving Cutter, Special Insert 3x 2777399
D44 Debug Cutter,Special Insert 3x 2777398
Notch Weldon Connect Grooving and Debug Cutter
The Solution:
High Precise Insert Guarantee Groove Width
The Results:
Grooving Debugrring
Vc 101 195 m/min
FPT 0.2 0.4 mm/rev
Z 3 3
STEEL

## Slide 41
小孔端面和倒角复合加工刀具
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Countersinking V-Sharp and Small Eye Chamfer
Coolant: Yes
Machine: M/C with 4 spindles
The Task:
HSK63A With Special Cartridge
2 Cartridge for Facing,1 Cartridge for Chamfer
Insert SCMT09T308MU TN8025
Axial Adjustable
The Solution:
D = 32 mm
Vc = 141 m/min
FPT = 0,08 mm/rev
Z=2
STEEL

## Slide 42
DWG 60052466
The Data:
Component: Pass. car conrod
Material: Powder Metal
Operation: Countersinking V-Shanp and Small Eye Chamfer
Coolant: Yes
Machine: M/C with 4 spindles
The Task:
HSK63A With Special Cartridge
2 Cartridge for Facing,1 Cartridge for Chamfer
Facing Insert CDE322L05 KC730
Axial Adjustable
The Solution:
D = 41 mm
Vc = 257 m/min (n=2000r/min)
FPT = 0,05 mm/rev
Z=2
Powder Metal
小孔端面和倒角复合加工刀具

## Slide 43
大小孔精加工刀具

## Slide 44
The Task:
Component: Conrod
Material: Powder Metal (HRC21~30, Tensile Strength 852MPa)
Operation: Finish Boring Conrod Small Eye
Coolant: Yes
Equipment: VMC BT40
The Solution:
Speical Romicron Boring Tool
Tight Tolerance, Romicron Easy setup
Short boring bar overhang(36mm) and tool length(145mm), Good Balance G2.5@5000rpm
Inset “CPGT060204LF KT315”
The Result:
Surface quality Ra0.8
Cylindrical 0.007-0.008mm
The Data:
Vc=200m/min Fz=0.08 Z=1
小孔精加工
Powder Metal

## Slide 45
大小孔精加工复合刀具
Romicron solution with individual micometric adjustment for both bores.
Insert CPMT060204LF KT315 for Crank Bore
Insert CPMT060204LF KC5010 for Piston Bore
The Solution:
piston Ø crank Ø
D = 58.033 +/-0.01 93.777 +/-0.013 mm
Vc = 40 400 m/min
FPT = 0,1 0,1 mm/rev
The Data:
Component: Truck conrod
Material: C70 S6 BY / BRONZE
Operation: Finishing piston and crankshaft bore
Coolant: Yes
Machine: HMC
The Task:
NON FERROUS
STEEL

## Slide 46
Used on a Pivot Head
HSK63A Special Tool with Cartriges
Insert SCMT09T308-11 HT93VX
Internal coolant
The Solution:
D = 50,6 mm
Vc = 250 m/min
Vf = 393 mm/min
FPT = 0,25 mm
The Data:
Component: Pass. car conrod
Material: C70 S6 BY
Operation: Fine boring
Coolant: Yes
Machine: Transferline
Objective: Surface finish and roundness
The Task:
大孔精加工
STEEL

## Slide 47
The Task:
Workpiece：Connecting Rod bushing
Material: ZCuSn10Zn2(HB90~110)
Operation: Fine boring pin bore ,before pressing the sintered bushing
Machine:Alfing 6 spindles horizontal MC
Objective:Achieve Surface finish cylindrical 0.005
The Solution:
Used on a Pivot Head,
Push boring the dia. 21.28,pull boring the dia. 22.009 and 22.029.
IP2811546 R4 big arc angle MKD insert machine the Elliptic and arch.
The Result:
Surface quality Ra0.8
Cylindrical within 0.005mm
The Data:
D1=21.28, D2=22.009~22.02993;
Zeff1=1, Zeff2=1.
Vc1 = 270 m/min, Vc2 = 280 m/min
fZ1 = 0.15 mm/rev, fZ2= 0.08 mm/rev
Doc1=0.5,Doc2=0.35
小孔精加工
NON FERROUS

## Slide 48
The Task:
Component: Conrod
Material: Powder Metal(HRC25-35,Tensile Strength 890 MPa)
Operation: Finish for Small Eye and Big Eye
Coolant: Internal Coolant
Equipment: 4 spindles HMC
The Solution:
D19.975/D47 RIQ Reamer, One tool finishing for Small and Big Eye.
RIQ Reamer, Easy Setup.
Cermet RIQ Insert(RIQ06R0400E01 SPA9NF), High cutting speed and High Tool Life.
Stock: Big Eye 0.2mm(Rad.),Small Eye 0.15mm
Assembly with “HSK63ASIF70066M”
The Result:
Roundness 0.005mm
Surface Roughness Ra0.8
The Data:
Vc=202m/min
Fz=0.145mm/r
Z=1
DWG 2702968
大小孔精铰加工
Powder Metal

## Slide 49
The Task:
Component: Truck Conrod
Material: C70S6BY
Operation: Finish Big Eye
Coolant: Internal Coolant
Equipment: Alfing 5 spindles
The Solution:
Semi-finishing and Finishing for Crank Bore
2x RIQ2757632 SPA9NF
The Result:
Cylindricity <0.006mm
The Data:
D1=18.75 D2=19
Z=1/1
Vc=190/190m/min
Fz=0.16/0.22mm/r
Doc=0.5/0.13
DWG 2757631
STEEL
小孔精加工（压套前）

## Slide 50
GDW 60133029
RIQ tool with SIF70 adaption, coupled to HSK63 backend
RIQ unit with Carbide guide pads
RIQ PCD insert in grade KD1415.
RIQ TOOL ASSY - RIQ60132092 [MM#5519312]
RIQ INSERT - RIQ06EGS00 [MM#5410390]
The Solution:
Bore roundness achieved is < 3µ
Cylindricity achieved is < 3µ
Surface achieved is 1Rz
The Results:
D = 22 mm
Vc = 291 m/min
Vf = 336 mm/min
FPT = 0,08 mm/rev
The Data:
Component: Pass. car conrod
Material: BRASS
Operation: Finishing piston bore
Coolant: Yes
Machine: M/C with mult spindles
Objective: Cylindricity < 6µ，Bore roundness < 4µSurface finish < 2.4Rz，Bore tolerance +/- 0.005µ
The Task:
NON FERROUS
小孔精加工（压套后）

## Slide 51
大头孔铰刀
The Task:
Operation: Reaming Big Eye
Coolant: Yes
Equipment: VMC BT40
The Solution:
Ø 94.993 RI8 Padded Reamer(DWG60255982)
Micro Cutting, Ø94.878 AND Ø94.993
Stock 0.4MM(DIA)
The Result:
Surface quality Ra0.8-1.2
The Data:
Vc=185m/min F=0.2mm/r
Notes: 铜的耐磨性好

## Slide 52
小头孔铰刀（压套前）
The Task:
Operation: Reaming Small Eye
Coolant: Yes
Equipment: VMC BT40
The Solution:
Ø 62.435 RI8 Padded Reamer (DWG60256961)
Micro Cutting, Ø62.421 AND Ø62.435
Stock 0.5MM(DIA)
The Result:
Surface quality Ra0.6-0.8
The Data:
Vc=235m/min F=0.1mm/r
Notes: 铜的耐磨性好

## Slide 53
小头孔铰刀（压套后）
The Task:
Operation: Reamer Small Eye
Coolant: Yes
Equipment: VMC BT40
The Solution:
Ø 58.056 RIR Padded Reamer(DWG60255977)
RIR R0.2 PCD Insert(DWG60231505),Grade:KD1415
Stock 0.4MM(DIA)
The Result:
Surface quality Ra0.6
Roundness<0.008mm
The Data:
Vc=300m/min F=0.19mm/r
Notes: 铜的耐磨性好

## Slide 54
Thank you
for your kind attention !
謝謝
肯纳亚洲（中国）企业管理有限公司
项目部 陈梓亮
zillion.chen@kennametal.com
M: +86 13701774770